Effect Of Interstitial Atom X On Structural, Elastic And Electronic Properties of NbRu3, NbXRu3     WITH (X= B  or C).

A. Benamer*1, A. Roumili#2, Y. Medkour #3, D. Maouche§4

* Department of Physics, Faculty of Sciences, University of Setif1, 19000 Setif, Algeria
# Laboratoire d’Etudes des Surfaces et Interfaces des Matériaux Solides (LESIMS), Université de Sétif1, Algérie.

§ Laboratory for Developing New Materials and their Characterizations, University of Setif1, Algeria.

1 benamer.ali2@yahoo.fr

2 rm_ab@yahoo.fr

3 you_med2000@yahoo.fr

4 djmaouche@yahoo.fr

Abstract— We report results obtained from first principle calculations of NbRu3, NbBRu3 and NbCRu3 compounds with antiperovskite structure. The estimated equilibrium lattice parameters are in agreement with the experimental ones. Elastic constants Cij for single crystal are calculated, then polycrystalline elastic moduli (bulk, shear and Young moduli, Poisson ration, anisotropy factor) are presented. Based on Debye model, Debye temperature ϴD is calculated from the sound velocities Vl, Vt and Vm. Band structure results show that the compounds under study are electrical conductors and the conduction mechanism is assured by Ru-d electrons. Bonding nature and bonds strength are discussed based on the partial densities of states, population analysis and the electronic charge distribution.

Keywords— Intermetallic compounds,  Ab initio calculations, Elastic properties

Introduction

Inverse-perovskites borides, carbides or nitrides have shown interesting and exceptional properties, like superconductivity [1, 2], negative thermal expansion [3, 4], giant magnetoresistance [5, 6] and high temperature resistant [7] . These compounds have the general formula M3AX [1] where X is either B, C or N. While both of M and A are metal atoms. The unit cell is cubic with M elements at 3c (1/2,1/2,0), A elements at 1a (0,0,0) and X elements at 1b (1/2,1/2,1/2). The interest to the antiperovskite AXM3 has been raised by the discovery of superconductivity for Ni3MgC at 8 K [8], nevertheless and then many experimental and theoretical studies were carried to investigate the origin of this behaviour [9]. Several studies were published on the synthesis of possible new borides based antiperovskite. Shaack et al. [10] have succeeded to fabricate many intermetallic perovskite borides and carbides in the ternary systems AXM3. The hardness as afunction of the continuous solid solution ScRh3BxC1-x was studied by Shishido et al. [11], they found that the microhardness increases with increasing boron content. In addition to the aforementioned experimental studies, theoretical works are carried out to accomplish the investigation of the physical properties of these antiperovskites compounds [12-20]. The study of the chemical bonding in roughly 20 boron-based antiperovskites RM3B shows an alternating covalent-ionic and metallic bonding in these compounds [12]. The substitution effect on electronic structure of MgXNi3 (X=B, C and N) was discussed [13], Electronic structure and lattice parameters of RPd3Bx (with R: rare earth metal) [14] and RRh3BxC1-x (R=Sc, Y) [15] were studied according to the boron content. Mechanical and optical properties of Sc3InX (X=B, C and N) [16]. Kellou et al. [17] reported a detailed work on structural and thermal properties of Fe3Al and Fe3AlX (X=H, B, C, N, O) compounds. They showed that C addition on Fe3Al has the highest effect of the strengthening cohesive energy, then the Fe3AlC is the most stable while Fe3AlH and Fe3AlO are relatively meta-stable. Using first principle method, A. Bouhemadou [18] has studied the pressure effect on the structural and elastic properties of RCRh3 (R=Sc, Y, La and Lu) up to 25 GPa  therefore numerical estimations of bulk modulus, shear modulus, Young's modulus, Poisson's ratio, Lame’s coefficients, average sound velocity and Debye temperature have been obtained for polycrystalline RCRh3. ACRu3 (A=V, Nb and Ta) have shown a good structural stability up to 50 GPa [19], according to the band structure calculations these compounds are electrical conductors and they are bonded by a mixture of covalent, ionic and metallic bonds. Depending on the type of A sublattices (A= Zn, Ca, Al, Ga, In, Ge, Hg, Sn, Cd, Pb, Ag, Sc, Ti, Y, Nb, Mo, and Ta), Pd- and Pt- based ternary carbides have demonstrated a rich variety of mechanical and electronic properties [20].

In this study, we report the effect of boron and carbon addition on the structural, elastic and electronic properties of NbRu3. These compounds have an inverse-perovskite structure, in which Nb atoms occupy primitive cubic sites, Ru atoms fill the fcc positions and B or C located at the bcc [1, 10]. After this introduction, the computational details were presented in section 2. In section 3, various results of NbRu3, NbBRu3 and NbCRu3 such as lattice parameters, single crystal elastic constant Cij, polycrystalline elastic moduli were discussed. In addition the electronic properties and chemical bonding are also investigated. This work was finished by a conclusion in section 4.

This document is a template.  An electronic copy can be downloaded from the conference website.  For questions on paper guidelines, please contact the conference publications committee as indicated on the conference website.  Information about final paper submission is available from the conference website.

I. CALCULATIONS METHOD

CASTEP (Cambridge Serial Total Energy Package) code [21] was used to perform this study. The problem of fundamental eigenvalue is resolved using the density functional theory [22] and the Kohn-Sham approach [23]. In the purpose of reducing the very important number of plane waves (PW), that’s describe the electron functions, a fictive potential (pseudopotential) is generated to replace the real atomic potential [24]. Pseudo atomic calculations were performed with; B: 2s22p1, C: 2s22p2; Nb: 4s24p6 4d45s1 and Ru: 4s24p6 4d75s1. Local density approximation LDA with the CA-PZ functional [25] was used to calculate the exchange correlation energy. The Broyden- Fletcher- Goldfarb- Shanno (BFGS) algorithm [26, 27] was used to find the fundamental energy of the crystal. After careful convergence tests, we have used 10x10x10 irreducible k points to sampling the first Brillouin zone sampling [28]. The ultra-soft pseudopotential was employed [24] with a cut off energy Ecut off = 380 eV. Calculations were done since the energy tolerance is about to 5.10-6 eV/atom, the maximum force is equal 0.01 eV/ Å, the maximum stress is lower than 0.02 GPa and a maximum displacement doesn’t exceed 5.10-4Å.

III. RESULTS AND DISCUSSION

A. Structural and elastic properties

Equilibrium lattice parameters of the studied compounds are listed in Table 1. We note the good agreement of our calculated lattice parameter a with the experimental ones [10], The deviation of calculated a from experimental ones varies from 1.3% for NbCRu3 up to 2% for NbBRu3. The addition of B and C atoms in the interstitial site (X) of NbRu3 increases the lattice constant by about 4.6% and 4.1% respectively. When substitute B by C atom the calculations show that the equilibrium volume of NbBRu3 goes from 64.08 Å3 to 63.18 Å3 for NbCRu3, i.e. a reduction of about 1.4%. This decrease might be related to the difference in the atomic radii of B (8.5 Å) and C (7 Å) where B radii is about 17% higher than the C radii.

TABLE I THE CALCULATED LATTICE CONSTANTS AND SINGLE CRYSTAL ELASTIC CONSTANTS.

|  |  | NbRu3 | NbBRu3 | NbCRu3 |
| --- | --- | --- | --- | --- |
| a (Å) | Our results Exp. [3] Other calc. [19] | 3.825 3.880 | 4.001 3.921 | 3.982 3.928 4.045 |
| v(Å3) | Our results | 55.98 | 64.08 | 63.18 |
| C11(GPa) | Our results Other calc. [19] | 477 | 634 | 600 546 |
| C44(GPa) | Our results Other calc. [19] | 202 | 160 | 155 150 |
| C12(GPa) | Our results Other calc. [19] | 228 | 137 | 187 187 |

Results of elastic constants Cij are carried out based on the finite elastic strain technique [29, 30]. Elastic stiffness of a cubic symmetry can be described using three independent elastic constants C11, C12 and C44 [29]. Our results for Cij are summarised in Table 1 with previous calculated data. The requirements for mechanical stability of the cubic system are [31]: C11-C12>0; C11+2C12>0 and C44>0, these requirements are fulfilled by the values reported in Table 1. The highest value is that of C11 which reflects the high stiffness along the principal directions in the cubic structure, the value of C11 is higher than the shear elastic modulus C44 by about 57% for NbRu3, 74% for both NbBRu3 and NbCRu3. By inserting B and C atoms in the interstitial sites X of NbRu3, C11 (C44) increases (decreases) by about 32% (20%) and 25% (23%) respectively. However the passage from NbBRu3 to NbCRu3 doesn’t affect considerably the values of C11 and C44. The observed overestimation between our results and those of Haddadi et al.[19] could be explained by the use of LDA, which well known to overestimate the elastic moduli of crystal as compared to the GGA [22].

Polycrystalline elastic constants are presented using only the Hill’s assumption, which is defined as the arithmetic average of the Voigt and Reuss approximations [29]. The bulk modulus B gives information about resistance to volume changes. However, shear modulus G provides information on shape change resistance [29]. Our results for the bulk modulus B, shear modulus G, tetragonal shear modulus G'= (C11 – C12)/2, Young’s modulus Y, Poisson’s ratio P, anisotropy factor A and Pugh’s criterion B/G for the ductility or brittleness are summarized in Table 2.

TABLE II POLYCRYSTALLINE ELASTIC MODULI; BULK MODULUS B; SHEAR MODULUS G; TETRAGONAL SHEAR MODULUS; YOUNG’S MODULUS E; POISSON’S RATIO P; ANISOTROPY COEFFICIENT A; PUGH’S CRITERION B/G; DENSITY Ρ; SOUND VELOCITIES VL, VT, VM AND DEBYE TEMPERATURE ΘD.

|  | NbRu3 | NbBRu3 | NbCRu3 |
| --- | --- | --- | --- |
| B(GPa) | 311 | 303 | 325; 307[19] |
| G(GPa) | 166 | 191 | 173; 161[19] |
| G’(GPa) | 124 | 248 | 206 |
| E(GPa) | 422 | 473 | 440; 412[19] |
| P | 0.2734 | 0.2395 | 0.2739; 0.2762[19] |
| A | 1.62 | 0.64 | 0.75; 0.839[19] |
| B/G | 1.87 | 1.58 | 1.87; 1.9[17] |
| ρ(gcm-3) | 11.7499 | 10.5447 | 10.7258; 10.4758[17] |
| Vl (ms-1) | 6730 | 7272 | 7197; 7085[19] |
| Vt(ms-1) | 3758 | 4255 | 4471; 3958[19] |
| Vm(ms-1) | 4184 | 4719 | 4471; 4407[19] |
| θD(K) | 445 | 480 | 457; 559[19] |

The bulk modulus of NbRu3 is 311GPa. When adding B atom to this compound, the bulk modulus decreases by about 2.5%, however, it increases by about 4.5% when inserting C atom.  According to our results, we observe an increase of the bulk modulus when going from NbBRu3 to NbCRu3, these results agree with the relation between the lattice parameter and the bulk modulus (B α 1/V) [32]. The resistance to shape change G is about 46% lower than the resistance to volume change B for NbRu3 and NbBRu3 and about 34% for NbCRu3. The highest resistance to shear deformation (G or G') is that of NbBRu3. Moreover, the sequence B>G>G' clearly demonstrates that the mechanical stability of the binary NbRu3 is limited by the tetragonal shear modulus G'. However, in the ternary NbBRu3 and NbCRu3 the mechanical stability is limited by the shear modulus G (i.e. B>G’>G). Our results for NbCRu3 are in good agreement with those reported in [19].

Young’s modulus E describes the behavior of a material versus one directional stress and gives a measure of the stiffness. NbBRu3 presents the higher stiffness, however NbRu3 presents the lower one. As reported by Haines et al. [33], a Poisson’s ratio of around 0.25 corresponds to predominate ionic bonding, while values around 0.33 reflect the presence of metallic bonding. The obtained values of 0.2395 < P < 0.2739 confirm the existence of ionic bonds in these compounds.

For isotropic materials A = 1, and any deviation of A from unity suggests the elastic anisotropy [29]. The obtained results show that the anisotropy factor deviates from the unity, then our compounds are all elastically anisotropic. The Pugh’s factor B/G expresses the malleability of a material. The B/G values higher than 1.75 indicate a ductile behavior, while the values lower 1.75 indicate brittleness [34]. Our calculated values of B/G for NbRu3 and NbCRu3 are slightly higher than the critical value separating brittleness from ductility, which is in good agreement with the low resistance to shear deformation. In opposite, NbBRu3 can be classified as brittleness compound with Pugh’s criterion of about 1.58. Note that there is a good agreement of our results with those reported in [19] for NbCRu3.

Based on Debye’s model [35], we have calculated the Debye’s temperature ϴD from the longitudinal Vl and the transversal Vt velocities of the elastic waves as shown in Table 2. Longitudinal wave velocity Vl is approximately 40% higher than Vt, and the average sound velocity Vm is inversely proportional to the density ρ. As compared to NbRu3, the density ρ of NbBRu3 (NbCRu3) increases by 10% (8.7%), while the Debye’s temperature decreases by 7.8% (2.6%). Therefore, and according to the relation between the melting temperature (Tm) and the Debye’s one (Tm α θD) [35], we can suggest that NbBRu3 has the higher melting temperature.

B. Electronic properties and chemical bonding

The calculated energy band structure at equilibrium lattice parameters for NbRu3, NbBRu3 and NbCRu3 along the high symmetry directions in the Brillouin zone is shown in Fig.1. It can be assessed that there is no gap at the Fermi level EF, at the vicinity of EF it exists an overlapping of bonding and antibonding states. As results NbRu3, NbBRu3 and NbCRu3 will exhibit metallic properties. At the Fermi level EF, the total density of state (TDOS) for NbRu3, NbBRu3 and NbCRu3, are 3.96, 1.43 and 3.36 (states / unit cell. eV) respectively. Thus there is an important decrease in the TDOS at EF from NbRu3 to NbBRu3. At lower energy level, the band structure of NbRu3 is formed from d electrons of Nb and Ru atoms.  Boron and Carbon didn’t contribute to the TDOS at the Fermi level and therefore are not included in the conduction properties. Ru-d electrons are mainly contributing to the TDOS at the Fermi level, and should be involved in the conduction properties. Valence band curves of NbBRu3 and NbCRu3 are moved to lowest energy level owing to more electronegativity of Boron and Carbon atoms. The valence band structure of NbBRu3 and NbCRu3 is formed from two parts. The lower part is derived from B-s, and Ru-d electrons. The upper section is derived from d electrons of Nb and Ru atoms. The conduction band is built from d states of Nb and Ru atoms, with a minor contribution from p states of Nb, Ru, B and C atoms.

To provide a deeper study on the bonding properties, we have studied the partial density of states. Fig.2 shows a strong hybridization of Ru-d and Nb-d states from -5 eV till Fermi level. We observed a forte hybridization Ru-d and B-p at -10 eV for NbBRu3, and Ru-d and C-p at -13 eV for NbCRu3, the later hybridization locates at deeper energy level, and then these bands are the stiffest in these compounds.

Fig. 1 Calculated band structure for NbRu3, NbBRu3 and NbCRu3.

To give a good comprehension of the bonding in these compounds, we have calculated the overlap population for nearest neighbors in the crystal (Table 3). Positive values express bonding states between atoms, while negative values show antibonding states [36, 37]. The present calculations reveal a positive overlapping population between Ru—Ru,    B—Ru and C—Ru bonds of NbRu3, NbBRu3 and NbCRu3 respectively, then the present bonds are in bonding state. Moreover, the high overlap value, the high degree of covalency in the bond [38]. According to the values reported in Table 3, these bonds are strong and of covalent type. On the other side, the difference in electronegativity between Ru, Nb , B and C atoms gives rise to a charge transfer and an ionic bonds will be occurred. Important charge transfer between Ru and Nb atoms causes a strong ionic bonding in NbRu3. For NbBRu3 and NbCRu3 the charge transfer from Nb atoms toward Ru is lessening, and then the ionic bonding is weakened. An important charge transfer from Nb towards both B and C atoms leads to a strong ionic bonding Ru—B and Ru—C. Strengthen Ru—B and Ru—C bonds and weaken Ru—Nb bonds give us a good explanation of the calculated bulk moduli for the under study compounds.

Fig. 2 Calculated total and partial density of states

(respectively TDOS and PDOS) for NbRu3, NbBRu3 and NbCRu3.

TABLE III BOND LENGTH AND OVERLAP POPULATION FOR NEAREST NEIGHBORS IN NbRb3, NbBRu3 AND NbCRu3.

| Compounds | Bonds | Bond length (Å) | Bond population (ǀeǀ) | Anion and cation charge (ǀeǀ) |
| --- | --- | --- | --- | --- |
| NbRu3 | Ru—Nb Ru— Ru | 2.70498 2.70498 | -0.26 0.42 | Ru: -0.18 Nb:0.57 |
| NbBRu3 | Ru— Nb Ru— Ru Ru—B | 2.82962 2.82962 2.00084 | 0.48 -0.41 0.50 | Ru: -0.05 Nb: 0.69 B:-0.54 |
| NbCRu3 | Ru—Nb Ru— Ru Ru— C | 2.81637 2.81637 1.99147 | 0.40 -0.49 0.55 | Ru: -0.04 Nb: 0.70 C:-0.58 |

We have extended our investigation of the chemical bonding to the charge density distribution in these compounds. We have illustrated the valence charge density in the upper panel for the (110) plane, and for (002) plane in the lower panel, as presented in Fig.3. For NbRu3 the electrons are shared between Ru and Nb atoms. For NbBRu3 and NbCRu3, we can observe a forte directional charge distribution along Ru—B and Ru—C directions, the electrons are shared between Ru—B and Ru—C atoms, which is a characteristic of the covalent bonds. It can be observed that Ru—B and Ru—C bonds are stronger than Ru—Ru bonds in NbRu3. Nb—Ru are less strong and of ionic nature, these results are in agreement with the observed hybridized states in Fig.2.

Fig. 3 Calculated charge density for NbRu3, NbBRu3 and NbCRu3.

IV. CONCLUSION

Based on first principle calculations, we have presented a study on the effect of interstitial atom X on structural, elastic, electronic properties of NbRu3, NbXRu3 (X=B and C). The calculated lattice parameters are in agreement with previous experimental and theoretical data. Elastic constant of single crystal Cij are in satisfactory agreement with the available theoretical data. Adding B and C atoms to NbRu3 increases the elastic stiffness. It was found that NbCRu3 has the higher bulk modulus, while NbBRu3 has the higher Young modulus, NbRu3 has the lower shear modulus. From the calculated band structure, total and partial densities of states, we have concluded that these compounds are good electrical conductors, where the electrical conductivity is assured by the Ru-d electrons.  The results show different hybridizations between Ru-d— (B/C)-p, Ru-d—Nb-d and Ru-d—Ru-d. From Mulliken analysis of the overlap population and the valence charge density, the bonds in these compounds are mixture of covalent, ionic and metallic.

REFERENCES

[1]: R. Ferro and A. Saccone, Intermetallic Chemistry, Elsevier, 2008.

[2]: S. Ram, V . Kanchana, Lattice dynamics and superconducting properties of antiperovskite La3InZ (Z = N,O) , Solid State Communications. 181 (2014)54-59.

[3]: AJ. Freeman, T. Jarlborg, Magnetism and superconductivity in rare-earth ternary borides, J. Appl. Phys. 50 (1979) 1876-1879.

[4]: P. Tong, Despina Louca, Graham King, Anna Llobet, J. C. Lin, and Y. P. Sun, Magnetic transition broadening and local lattice distortion in the negative thermal expansion antiperovskite Cu1-xSnxNMn3, Appl. Phys. Lett. 102 (2013)041908-041911.

[5]: X. H. Zhang, Y.Yin, Q.Yuan, et al., Magnetoresistance reversal in antiperovskite compound Mn3Cu0.5Zn0.5N, J. Appl. Phys. 115 (2014)123905-123909.

[6]: Tong Peng, Wang Bo-Sen, Sun Yu-Ping, Mn-based antiperovskite functional materials: Review of research. Chinese Physics B 22 (2013) 067501-067513.

[7]: M. D. Alvey and P. M. George, ZrPt3 as a high-temperature, reflective, oxidation-resistant coating for carbon-carbon composites. Carbon  29 (1991) 523-530.

[8]: T. He, Q. Huang, A. P. Ramirez, Y. Wang, K. A. Regan, N. Rogado, M. A. Hayward, M. K. Hass, J.S. Slusky, K. Inumara, H. W. Zandbergen, N. P. Ong, and R. J. Cava, Superconductivity in the non-oxide perovskite MgCNi3.Nature. 411 (2001) 54- 56.

[9]: S. Mollah, The physics of the non-oxide perovskite superconductor MgCNi3. J. Phys. Condens. Matter. 16 (2004) R1237-R1276.

[10]: R. E. Schaack, M. Avdeev, W. L. Lee, G. Lawes, H. W. Zandbergen, J. D. Jorgensen, N.  P. Ong, A. P. Ramirez, and R. J. Cava, Formation of transition metal boride and carbide perovskites related to superconducting MgCNi3. J. Solid State Chem. 177 (2004) 1244- 1251.

[11] :  T. Shishido, J. Ye, K. Kudou, S. Okada, K. Iizumi, M. Oku, Y. Ishizawa, A. Yoshikawa, M. Tanaka, A. Nomura, T. Sugawara, K. Obara, T. Amano, S. Oishi, N. Kamegashira ,Y. Kawazoe, S. Kohiki, K. Nakajima, Boron–carbon atomic ratio dependence on the hardness and oxidation resistance of perovskite-type solid solution ScRh3BxC1−x . Journal of Alloys and Compounds 375 (2004) 217–220.

[12] : D. Music,  Z. Sun, and Jochen M. Schneider, Alternating covalent-ionic and metallic bonding in perovskite borides studied using ab initio methods   , Phys. Rev. B 71 (2005) 052104 -52106.

[13]: J. H. Shim, S. K. Kwon, and B. I. Min, Electronic structures of antiperovskite superconductors MgXNi3 .X=B, C, and N. Phys. Rev. B. 64 (2001) 180510-180513.

[14]: C. Loison, A. Leithe-Jasper, and H. Rosner, Electronic structures of intermetallic borides RPd3Bx (R=rare-earth metals), Phys. Rev. B 75 (2007) 205135-205143.

[15]: R Sahara, T. Shishido, A. Nomura, K. Kudou, S. Okada, V. Kumar , First-principles study of the structural, electronic, and elastic properties of RRh3BxC1−x (R=Sc and Y), Phys. Rev. B 76 (2007) 024105-024113.

[16]: M. A. Hossain, M. S. Ali, F. Parvin, A.K. M. A. Islam, Mechanical and optical properties of inverse-perovskite Sc3InX (X=B, C, N), Comp. Mater. Sci., 73, 1-8, 2013.

[17]: A. Kellou, J. M.Raulot, T. Grosdidier, Structural and thermal properties of Fe3Al, Fe3AlC and hypothetical Fe3AlX (X = H, B,N,O)compounds: Ab initio and quasi-harmonic Debye modelling, Intermetallics 18 (2010)1293-1296

[18]: A. Bouhemadou, Elastic properties of mono- and polycrystalline RCRh3 (R = Sc; Y; La and Lu) under pressure effect, Solid State Communications 149 (2009) 1658-1662.

[19]: K. Haddadi, A. Bouhemadou, L. Louail, M. Maamache, Density functional study of the structural, electronic, elastic and thermodynamic properties of ACRu3 (A = V, Nb and Ta) compounds, Intermetallics 19 (2011) 476-485.

[20]: V.V. Bannikov, A.L. Ivanovskii, Elastic and electronic properties of antiperovskite-type Pd- and Pt-based ternary carbides from first-principles calculations, J. Alloys Compd. 577 (2013) 615–621.

[21]: M. D. Segall, P. J. D Lindan, M. J. Probert, C. J. Pickard, P. J. Hasnip, S. J. Clark and        M. C. Payne, First-principles simulation: ideas, illustrations and the CASTEP code, J. Phys : Condens. Matter, 14 (2002) 2717-2744.

[22]: J. Kohanoff, Electronic structure calculations for solids and molecules, Cambridge University Press, 2006.

[23]: W. Kohn, L. J. Sham, Self-consistent equations including exchange and correlation effects, Phys. Rev. A 140 (1965)1133-1138.

[24]:  M. C. Payne, M. P. Teter, D. C. Allan, T. A.  Arias and J. D. J. Joannopoulos, Iterative

minimization techniques for ab initio total-energy calculations: molecular dynamics and conjugate gradients, Rev. Mod. Phys., 64 (1992) 1045-1097.

[25]: D. M. Ceperley, B. J. Alder, Ground state of the electron gas by a stochastic method, Phys. Rev. Lett., 45 (1980) 566-569.

[26]: B. G. Pfrommer, M. Cote, S. G. Louie, M. L. Cohen, Relaxation of Crystals with the Quasi-Newton Method .J. Comput. Phys. 131 (1997) 233-240.

[27]: S. J. Clark, M. D. Segall, C. J. Pickard, P. J. Hasnip, M. J. Probert, K. Refson and          M. C. Payne, First principles methods using CASTEP, Z. Kristallogr., 220 (2005) 567- 570.

[28]: H. J. Monkhorst and J. D. Pack, Special points for Brillouin-zone integrations, Phys. Rev., B. 13 (1976) 5188- 5192.

[29]: E. Schreiber, O.L. Anderson, N. Soga, Elastic Constants and Their Measurement, McGraw-Hill, New York, 1973.

[30]: V. Milman, M. C.Warren, Elastic properties of TiB2 and MgB2. J. Phys.: Condens. Matter, 13, (2001) 5585-5595.

[31]: J. Wang, S. Yip, SR. Phillpot, D. Wolf. Crystal instabilities at finite strain. Phys. Rev. Lett. 71 (1993) 4182–4185.

[32]: M. L. Cohen, Calculation of bulk moduli of diamond and zincblende solids . Phys. Rev. B 32 (1985) 7988-7991.

[33]: J. Haines, J. M. Léger, and G. Bocquillon, Synthesis and design of superhard materials. Annu. Rev. Mater. Res. 31 (2001) 1–23.

[34]: S. F. Pugh, Relations between the elastic moduli and the plastic properties of polycrystalline pure metals. Philos. Mag. 45 (1954) 823-843.

[35]: J. P. Poirier, Introduction to the physics of the earth's interior, Cambridge University Press, Second edition 2000.

[36]: M. D. Segall, R. Shah, C.J. Pickard, M.C. Payne, Population analysis of plane-wave

electronic structure calculations of bulk materials, Phys. Rev. B. 54 (1996) 16317–16320.

[37]:  M.D. Segall, Population analysis in plane wave electronic structure calculations, Mol. Phys. 89 (1996) 571–575.