SYNTHESIS OF THE CuInSe2 THIN FILMS FOR SOLAR CELLS USING SHS TCHNIQUE AND THERMAL EVAPORATION

L. Saad Hamideche a,*, A. Amara a, F; Boutarfa b, A.Boussoukssou c, A. Benaldjia a, A. Drici a, N. Benslimd.

a Laboratoire d’Etude et de Recherche des Etats Condensés (LEREC), Département de Physique, Faculté des Sciences, Université Badji Mokhtar , Annaba, Algérie

bComplex of  Arcielor Metal  of Elhadjar, Annaba , Algeria.

c LAMP, Université de Nantes, 2 Rue de Hossinnière,  BP 92208. Nantes CEDEX 3, 44322, FRANCE.

d Laboratoire d’Etude de Surfaces et Interfaces de la Matière Solide (LESIMS), Département de Physique, Faculté des Sciences, Université Badji Mokhtar, Annaba, Algérie.

* Département de Physique, Faculté des Sciences, Université Mentouri, Constantine, Algérie.

Abstract: The samples of semi conductors of CuInSe2 were prepared by self propagating high temperature synthesis (SHS) and direct thermal evaporation onto pr-cleaned glass substrates, using a BALZERS coating unit. The as deposited films were annealed in a vacuum at different temperatures. The structural characterization of the as-deposited CuInSe2 films of various thicknesses has been carried out by X-ray diffraction method. The diffractogram revealed that the CuInSe2 films are polycrystalline in nature with chalcopyrite structure. The surface morphology of the as-deposited CuInSe2 thin films has been studied using scanning electron microscope. The transmittance characteristics of the CuInSe2 films have been studied using double beam spectrophotometer in the wavelength range 4000–15000A°. The absorption coefficient has been found to be very high and is of the order of 105–106 m-1. CuInSe2 films are found to have a direct allowed transition and the optical band gap is found to be in the range 0.85–1.05 eV.

Key words: Conversion photovoltaic, CuInSe2, optical properties, Absorption coefficient.

References:

[1 J.Müller, J.Nowoczin, Schimitt. Thin Solid Films 496 364-370 (2006).

[2]	C.Calderon, G.Gordillo, E.Romero, W.Bolaños, and P. Bartolo-Pérez, Phys. Stet, Sol. (b) 242, N°. 9, 1910-1914 (2005).